FERROCHROME KPI FRAMEWORK

Complete Reference Guide

Plant Language Meanings & Python Formulas

(Per Ton / Per Batch Basis)

BALASORE ALLOYS LIMITED

IT Department - Business Intelligence

Document Version: 2.0 | January 2025

# TABLE OF CONTENTS

- Introduction & Data Structure

- Charge Mix & Blending KPIs

- Alloy Quality KPIs

- Slag Chemistry KPIs

- Process Efficiency KPIs

- Cost & Economic KPIs

- Moisture & Power Relationship

- Target Specifications & Constraints

- Complete Python Class Implementation

- Quick Reference Tables

# 1. INTRODUCTION & DATA STRUCTURE

This document provides a complete KPI framework for Ferrochrome production at Balasore Alloys Limited. Each KPI includes plant-level meaning (what operators understand) and exact Python code for calculation.

## 1.1 Blending Logic at Balasore Ferrochrome Plant

At the Balasore ferrochrome plant, blending is a controlled and systematic process used to decide the quantity of each raw material (ore, flux, and reductant) charged into the submerged arc furnace. The objective of blending is to achieve customer-specified alloy chemistry, stable furnace operation, acceptable slag chemistry, and minimum overall cost.

## 1.2 Basic Material Parameters Used in Blending

Each raw material is defined by key parameters:

| Parameter | Target Value |
| --- | --- |
| Material | Name of raw material |
| Quantity | Weight in kg |
| Cr2O3 | Chromium oxide % |
| Cr | Chromium metal % |
| Fe | Iron % |
| SiO2 | Silica % |
| P | Phosphorus % |
| S | Sulphur % |
| Al2O3 | Alumina % |
| CaO | Calcium oxide % |
| MgO | Magnesium oxide % |
| FC | Fixed Carbon % |
| H2O | Moisture % |
| Rate | Cost per unit (Rs/kg) |

## 1.3 Customer and Furnace Targets (58/4 Grade)

Metal Chemistry Targets:

| Parameter | Target Value |
| --- | --- |
| Cr (Chromium) | 58 to 61 |
| Si (Silicon) | ≤ 4% |
| C (Carbon) | ≤ 8.5% |
| P (Phosphorus) | ≤ 0.03% |
| S (Sulphur) | ≤ 0.05% |

Slag Chemistry Targets:

| Parameter | Target Value |
| --- | --- |
| Cr2O3 | ≤ 8% |
| FeO | ≤ 2% |
| SiO2 | ≤ 28% |
| Al2O3 | ≤ 25% |
| CaO | ≤ 8% |
| MgO | ≤ 27% |
| Slag Basicity | 1.25 |
| Slag Ratio | 1.15 |

## 1.4 Input Data Structure

Purpose: Standard DataFrame structure for all calculations

import pandas as pd import numpy as np # Required DataFrame Columns: # Material ¦ Weight_kg ¦ Cr2O3 ¦ Fe ¦ SiO2 ¦ Al2O3 ¦ CaO ¦ MgO ¦ FC ¦ H2O ¦ Rate df = pd.DataFrame({ 'Material': ['MG_ORE', 'SHG_ORE', 'COKE', 'FLUX'], 'Weight_kg': [400, 300, 150, 50], 'Cr2O3': [42.5, 48.2, 0, 0], 'Fe': [16.8, 14.2, 0.5, 0.3], 'SiO2': [8.5, 6.2, 5.0, 2.0], 'Al2O3': [12.0, 10.5, 3.0, 1.0], 'CaO': [0, 0, 0.5, 45.0], 'MgO': [18.0, 20.0, 0.2, 5.0], 'FC': [0, 0, 85.0, 0], 'H2O': [3.5, 2.8, 8.0, 1.0], 'Rate': [8500, 12000, 15000, 3500] })

# 2. CHARGE MIX & BLENDING KPIs

These KPIs calculate the weighted average composition of raw materials charged into the furnace.

## 2.1. Blended Cr₂O₃ (%)

Plant Meaning: The average chromium oxide content in the ore mix going into furnace. Higher Cr2O3 means richer ore and more metal output per batch.

Why It Matters: Directly controls alloy production rate and recovery efficiency.

Target Range: 38-48% depending on ore grade mix

Formula:

Weighted average of Cr2O3 across all materials

Python Implementation:

df['Cr2O3_contrib'] = df['Weight_kg'] * df['Cr2O3'] blended_Cr2O3 = df['Cr2O3_contrib'].sum() / df['Weight_kg'].sum() # Result: Percentage (e.g., 42.5%)

## 2.2. Blended Cr (%) - Theoretical Chromium

Plant Meaning: The actual chromium metal available for reduction. Cr2O3 contains 68.4% Cr by stoichiometry.

Why It Matters: This is what actually becomes metal in your alloy.

Target Range: Conversion Factor: 0.684 (from molecular weight ratio: 2×52 / 152)

Formula:

Blended_Cr = Blended_Cr2O3 × 0.684

Python Implementation:

# Convert Cr2O3 to elemental Cr blended_Cr = blended_Cr2O3 * 0.684 # Result: Percentage of Cr available (e.g., 29.1%)

## 2.3. Blended Fe (%)

Plant Meaning: Iron content in the charge mix. Iron also reduces and reports to metal.

Why It Matters: Affects Cr/Fe ratio in final alloy and total metal recovery.

Target Range: 14-18% typically

Formula:

Weighted average of Fe

Python Implementation:

df['Fe_contrib'] = df['Weight_kg'] * df['Fe'] blended_Fe = df['Fe_contrib'].sum() / df['Weight_kg'].sum() # Result: Percentage (e.g., 15.8%)

## 2.4. Blended SiO₂ (%)

Plant Meaning: Silica is the main slag former. It consumes power and creates slag volume.

Why It Matters: Higher SiO2 = more power consumption, more slag, lower recovery.

Target Range: 6-10% (lower is better)

Formula:

Weighted average of SiO2

Python Implementation:

df['SiO2_contrib'] = df['Weight_kg'] * df['SiO2'] blended_SiO2 = df['SiO2_contrib'].sum() / df['Weight_kg'].sum() # Result: Percentage (e.g., 7.5%)

## 2.5. Blended Al₂O₃ (%)

Plant Meaning: Alumina controls slag viscosity. Too much makes slag thick and hard to tap.

Why It Matters: Affects slag fluidity and furnace operation.

Target Range: 8-14%

Formula:

Weighted average of Al2O3

Python Implementation:

df['Al2O3_contrib'] = df['Weight_kg'] * df['Al2O3'] blended_Al2O3 = df['Al2O3_contrib'].sum() / df['Weight_kg'].sum() # Result: Percentage (e.g., 11.2%)

## 2.6. Blended CaO (%) - From Flux

Plant Meaning: Lime from flux materials. Controls slag basicity.

Why It Matters: Affects sulphur removal and slag chemistry.

Target Range: Source: Mainly from limestone/dolomite flux

Formula:

CaO contribution from flux materials only

Python Implementation:

flux_df = df[df['CaO'] > 0] blended_CaO = (flux_df['Weight_kg'] * flux_df['CaO']).sum() / df['Weight_kg'].sum() # Result: Percentage (e.g., 2.5%)

## 2.7. Blended MgO (%)

Plant Meaning: Magnesia from ore and flux. Protects furnace lining and controls slag.

Why It Matters: Critical for refractory life and slag melting point.

Target Range: 15-22%

Formula:

Weighted average of MgO from all sources

Python Implementation:

df['MgO_contrib'] = df['Weight_kg'] * df['MgO'] blended_MgO = df['MgO_contrib'].sum() / df['Weight_kg'].sum() # Result: Percentage (e.g., 18.5%)

## 2.8. Fixed Carbon - FC (kg/ton)

Plant Meaning: The actual carbon available for reduction from coke/coal. This is the 'fuel' that reduces oxide to metal.

Why It Matters: Insufficient FC = incomplete reduction = Cr loss to slag.

Target Range: 380-450 kg FC per ton alloy

Formula:

Total FC from carbon-bearing materials

Python Implementation:

carbon_df = df[df['FC'] > 0] FC_kg = (carbon_df['Weight_kg'] * carbon_df['FC']).sum() / 100 # Result: kg of fixed carbon (e.g., 127.5 kg per batch)

## 2.9. Moisture - H₂O (kg/ton)

Plant Meaning: Water content wastes power (700 kWh/ton water evaporated). Every kg moisture = lost production.

Why It Matters: Directly increases specific power consumption.

Target Range: Minimize - typically 3-6%

Formula:

Total moisture load

Python Implementation:

H2O_kg = (df['Weight_kg'] * df['H2O']).sum() / 100 # Result: kg of moisture (e.g., 35 kg per batch)

## 2.10. Blended Charge Cost (₹/ton)

Plant Meaning: True weighted cost of raw materials per ton of charge.

Why It Matters: Direct input to alloy costing and margin calculation.

Formula:

Weighted cost per ton

Python Implementation:

blended_cost = (df['Weight_kg'] * df['Rate']).sum() / 1000 # Result: Rs per ton of charge (e.g., ₹9,250/ton)

# 3. ALLOY QUALITY KPIs

These KPIs measure the quality of the final ferrochrome alloy produced.

## 3.1. Grade Cr (%) - Chromium in Alloy

Plant Meaning: The chromium percentage in final alloy. This determines the GRADE (HC FeCr, MC FeCr, LC FeCr).

Why It Matters: Directly determines selling price and customer acceptance.

Target Range: HC: 60-70% Cr, MC: 56-65% Cr, LC: 60-65% Cr

Formula:

Based on metal recovery

Python Implementation:

Cr_recovered_kg = blended_Cr * Cr_recovery * total_charge_kg / 100 Fe_recovered_kg = blended_Fe * Fe_recovery * total_charge_kg / 100 Grade_Cr = (Cr_recovered_kg / (Cr_recovered_kg + Fe_recovered_kg)) * 100 # Result: Percentage (e.g., 62.5% Cr)

## 3.2. Cr/Fe Ratio

Plant Meaning: Quality indicator - higher ratio means premium grade alloy.

Why It Matters: Customer specification requirement. Affects pricing tier.

Target Range: 2.8-4.5 depending on grade

Formula:

Cr / Fe ratio

Python Implementation:

Cr_Fe_ratio = Grade_Cr / (100 - Grade_Cr - Si_percent - C_percent) # Simplified: Cr_Fe_ratio = Cr / Fe # Result: Ratio (e.g., 3.2)

## 3.3. Silicon in Alloy (%)

Plant Meaning: Silicon that reduced and entered the metal. Some SiO2 reduces to Si at high temperature.

Why It Matters: Specification limit. Too high Si = off-grade product.

Target Range: 1-4% for HC grade

Formula:

SiO2 × 0.467 × reduction_factor (typically 15% reduces)

Python Implementation:

reduction_factor = 0.15 # 15% of SiO2 reduces to Si Si_percent = blended_SiO2 * 0.467 * reduction_factor # 0.467 = molecular weight ratio (Si/SiO2 = 28/60) # Result: Percentage (e.g., 2.1%)

## 3.4. Phosphorus in Alloy (%)

Plant Meaning: Harmful element that cannot be removed during smelting. Comes from ore.

Why It Matters: Strict specification limit. High P = rejected alloy.

Target Range: < 0.03% for quality grades

Formula:

~90% of input P reports to metal

Python Implementation:

P_percent = P_input * 0.90 # Result: Percentage (e.g., 0.025%)

## 3.5. Sulphur in Alloy (%)

Plant Meaning: Comes from coke/coal. Partially removed by slag.

Why It Matters: Quality specification. High S = quality downgrade.

Target Range: < 0.05% for quality grades

Formula:

~85% of input S reports to metal

Python Implementation:

S_percent = S_input * 0.85 # Result: Percentage (e.g., 0.04%)

## 3.6. Cr + Fe (%) - Total Reducible Metal

Plant Meaning: The total metal content that will be reduced. This is your potential alloy yield.

Why It Matters: Higher Cr+Fe = more metal per batch.

Target Range: 42-50%

Formula:

Sum of reducible metals

Python Implementation:

Cr_Fe_total = blended_Cr + blended_Fe # Result: Percentage (e.g., 44.9%)

# 4. SLAG CHEMISTRY KPIs

Slag chemistry determines furnace operation, recovery, and refractory life.

## 4.1. Slag Cr₂O₃ (%) - Chromium Loss

Plant Meaning: Chromium lost to slag = money lost. Lower is better.

Why It Matters: Direct measure of recovery efficiency. 1% slag Cr2O3 = significant Cr loss.

Target Range: < 6-8% Cr2O3 in slag

Formula:

Unreduced Cr2O3 goes to slag

Python Implementation:

Cr_recovery = 0.88 # 88% typical recovery Slag_Cr2O3_percent = blended_Cr2O3 * (1 - Cr_recovery) * slag_factor # Result: Percentage in slag (e.g., 7.2%)

## 4.2. Slag SiO₂ (%)

Plant Meaning: Most SiO2 reports to slag. Determines slag volume and viscosity.

Why It Matters: Controls slag fluidity and tapping behavior.

Target Range: 28-35% in slag

Formula:

~85-95% of SiO2 goes to slag

Python Implementation:

slag_SiO2_factor = 0.90 Slag_SiO2_percent = blended_SiO2 * slag_SiO2_factor / slag_ratio # Result: Percentage in slag (e.g., 32%)

## 4.3. MgO/Al₂O₃ Ratio - Slag Fluidity Index

Plant Meaning: Controls slag viscosity. High ratio = more fluid slag.

Why It Matters: Fluid slag taps easily, thick slag causes operational problems.

Target Range: 1.2-1.8

Formula:

MgO / Al2O3

Python Implementation:

MgO_Al2O3_ratio = blended_MgO / blended_Al2O3 # Result: Ratio (e.g., 1.65)

## 4.4. (MgO + CaO)/SiO₂ - Basicity Index

Plant Meaning: Slag basicity controls sulphur removal and refractory attack.

Why It Matters: Too acidic = refractory attack. Too basic = high melting point.

Target Range: 1.0-1.4 for optimal operation

Formula:

(MgO + CaO) / SiO2

Python Implementation:

Basicity = (blended_MgO + blended_CaO) / blended_SiO2 # Result: Ratio (e.g., 1.25)

## 4.5. Slag Volume (kg/ton alloy)

Plant Meaning: Total slag generated per ton of alloy. More slag = more handling cost.

Why It Matters: Affects furnace capacity and slag disposal cost.

Target Range: 800-1200 kg slag per ton alloy

Formula:

Sum of slag-forming oxides

Python Implementation:

slag_forming = blended_SiO2 + blended_Al2O3 + blended_CaO + blended_MgO slag_kg = (slag_forming / 100) * total_charge_kg Slag_per_ton_alloy = slag_kg / alloy_produced_ton # Result: kg per ton alloy (e.g., 1050 kg)

## 4.6. SiO₂/(Cr+Fe) - Power & Slag Indicator

Plant Meaning: Ratio of gangue to metal. Higher ratio = more power needed per ton metal.

Why It Matters: Key indicator for specific power consumption.

Target Range: < 0.20 for efficient operation

Formula:

SiO2 / (Cr + Fe)

Python Implementation:

SiO2_CrFe = blended_SiO2 / Cr_Fe_total # Result: Ratio (e.g., 0.167)

# 5. PROCESS EFFICIENCY KPIs

These KPIs measure how efficiently the furnace converts inputs to outputs.

## 5.1. Chromium Recovery (%)

Plant Meaning: How much of input Cr actually becomes metal. The single most important efficiency KPI.

Why It Matters: 1% recovery improvement = significant revenue increase.

Target Range: 85-92%

Formula:

Output Cr / Input Cr

Python Implementation:

Cr_input_kg = blended_Cr * total_charge_kg / 100 Cr_output_kg = alloy_kg * alloy_Cr_percent / 100 Cr_recovery = (Cr_output_kg / Cr_input_kg) * 100 # Result: Percentage (e.g., 88.5%)

## 5.2. FC/(Cr+Fe) - Carbon Sufficiency Index

Plant Meaning: Is there enough carbon to reduce all the metal? This ratio indicates carbon balance.

Why It Matters: Low ratio = incomplete reduction = Cr loss to slag.

Target Range: 0.85-1.05

Formula:

FC_kg / (Cr+Fe metal kg)

Python Implementation:

FC_CrFe = FC_kg / (Cr_Fe_total * total_charge_kg / 100) # Result: Ratio (e.g., 0.92)

## 5.3. Specific Cr Ore (kg ore/ton alloy)

Plant Meaning: How much ore needed to make one ton of alloy.

Why It Matters: Lower is better - indicates efficient ore utilization.

Target Range: 2200-2800 kg ore per ton alloy

Formula:

Ore consumption per ton alloy

Python Implementation:

ore_df = df[df['Cr2O3'] > 0] # Identify ore materials Sp_Cr_ore = ore_df['Weight_kg'].sum() / alloy_produced_ton # Result: kg per ton alloy (e.g., 2450 kg)

## 5.4. Specific Carbon (kg carbon/ton alloy)

Plant Meaning: Carbon consumption per ton alloy produced.

Why It Matters: Higher than optimal = wastage, lower = incomplete reduction.

Target Range: 380-450 kg per ton alloy

Formula:

FC_kg / alloy_produced_ton

Python Implementation:

Sp_Carbon = FC_kg / alloy_produced_ton # Result: kg per ton alloy (e.g., 410 kg)

## 5.5. Batch Volume (m³)

Plant Meaning: Physical volume of charge going into furnace.

Why It Matters: Must fit in furnace. Affects charging time and feeding.

Formula:

Weight / Bulk density

Python Implementation:

bulk_density = 1800 # kg/m³ typical for charge mix Batch_volume = total_charge_kg / bulk_density # Result: Cubic meters (e.g., 0.55 m³)

## 5.6. Specific Power (kWh/ton alloy)

Plant Meaning: Electricity consumed per ton of alloy. Biggest operating cost.

Why It Matters: Power is 40-50% of production cost.

Target Range: 3400-3800 kWh/ton for efficient furnace

Formula:

Total power / alloy produced

Python Implementation:

Sp_Power = total_power_kWh / alloy_produced_ton # Result: kWh per ton (e.g., 3550 kWh/ton)

# 6. COST & ECONOMIC KPIs

These KPIs track the economics of ferrochrome production.

## 6.1. Ore Cost (₹/ton alloy)

Plant Meaning: Cost of chrome ore per ton of alloy produced.

Why It Matters: Typically 30-40% of total cost.

Formula:

Weighted ore cost per ton alloy

Python Implementation:

ore_df = df[df['Cr2O3'] > 0] Ore_cost = (ore_df['Weight_kg'] * ore_df['Rate']).sum() / alloy_produced_ton # Result: Rs per ton alloy (e.g., ₹25,000/ton)

## 6.2. Reductant Cost (₹/ton alloy)

Plant Meaning: Cost of coke/coal/LAMC per ton of alloy.

Why It Matters: Typically 15-25% of total cost.

Formula:

Weighted reductant cost per ton alloy

Python Implementation:

carbon_df = df[df['FC'] > 0] Reductant_cost = (carbon_df['Weight_kg'] * carbon_df['Rate']).sum() / alloy_produced_ton # Result: Rs per ton alloy (e.g., ₹12,000/ton)

## 6.3. Flux Cost (₹/ton alloy)

Plant Meaning: Cost of flux materials (dolomite, quartz, etc.).

Why It Matters: Small but necessary cost component.

Formula:

Weighted flux cost per ton alloy

Python Implementation:

flux_df = df[df['CaO'] > 0] Flux_cost = (flux_df['Weight_kg'] * flux_df['Rate']).sum() / alloy_produced_ton # Result: Rs per ton alloy (e.g., ₹1,500/ton)

## 6.4. Power Cost (₹/ton alloy)

Plant Meaning: Electricity cost per ton of alloy.

Why It Matters: Biggest single cost element (40-50%).

Formula:

Specific Power × Power Rate

Python Implementation:

power_rate = 6.50 # Rs per kWh Power_cost = Sp_Power * power_rate # Result: Rs per ton alloy (e.g., ₹23,000/ton)

## 6.5. Total Production Cost (₹/ton alloy)

Plant Meaning: Complete cost to produce one ton of alloy.

Why It Matters: Determines profitability and competitiveness.

Formula:

Sum of all costs

Python Implementation:

Total_cost = Ore_cost + Reductant_cost + Flux_cost + Power_cost # Result: Rs per ton alloy (e.g., ₹52,000/ton)

# 7. MOISTURE & POWER RELATIONSHIP

## 7.1 What is H₂O / Moisture in Blending?

H₂O (Moisture) = Water present in Ores, Fluxes, and Reductants. Measured as % moisture by weight.

## 7.2 Why Moisture Increases Power Consumption?

Because water must be evaporated first before smelting. This requires energy for: (1) Heat water from ambient to 100°C, (2) Evaporate it (latent heat), (3) Superheat steam in furnace. All this consumes electrical power.

## 7.3 Industry Rule of Thumb

1 kg moisture consumes ~0.6 to 0.8 kWh of power

Industry standard approximation: 0.7 kWh per kg H₂O

## 7.4 Moisture Calculation

# Moisture Calculation (per ton charge) H2O_kg = sum(Material_weight_kg * Moisture_percent) / 100 # Power loss due to moisture Power_H2O = H2O_kg * 0.7 # kWh # Total Power with moisture penalty Power_per_ton = Base_Power + (H2O_kg * 0.7)

## 7.5 Example Calculation

| Parameter | Target Value |
| --- | --- |
| Ore A (600 kg, 4% moisture) | 24 kg H₂O |
| Ore B (300 kg, 6% moisture) | 18 kg H₂O |
| Flux (100 kg, 2% moisture) | 2 kg H₂O |
| Total Moisture | 44 kg |
| Power Penalty (44 × 0.7) | 30.8 kWh |
| If Base Power = 3400 kWh | Total = 3431 kWh/ton |

# 8. TARGET SPECIFICATIONS & CONSTRAINTS

## 8.1 Python Target Specifications (58/4 Grade)

# FINAL METAL SPECIFICATION (58/4) TARGET_METAL_SPEC = { "Cr_min": 57.5, "Cr_max": 58.5, "Si_max": 4.0, "C_max": 8.5, "P_max": 0.03, "S_max": 0.05 } # SLAG CHEMISTRY SPECIFICATION TARGET_SLAG_SPEC = { "Cr2O3_max": 8.0, "FeO_max": 2.0, "SiO2_max": 28.0, "Al2O3_max": 25.0, "CaO_max": 8.0, "MgO_max": 27.0 } # SLAG RATIOS TARGET_RATIOS = { "slag_ratio": 1.15, # (MgO + CaO) / SiO2 "basicity": 1.25 # CaO / SiO2 }

## 8.2 Constraint Checking Function

def check_constraints(metal, slag): """ metal = dict with keys: Cr, Si, C, P, S slag = dict with keys: Cr2O3, FeO, SiO2, Al2O3, CaO, MgO """ # Metal constraints metal_ok = ( TARGET_METAL_SPEC["Cr_min"] <= metal["Cr"] <= TARGET_METAL_SPEC["Cr_max"] and metal["Si"] <= TARGET_METAL_SPEC["Si_max"] and metal["C"] <= TARGET_METAL_SPEC["C_max"] and metal["P"] <= TARGET_METAL_SPEC["P_max"] and metal["S"] <= TARGET_METAL_SPEC["S_max"] ) # Slag constraints slag_ok = ( slag["Cr2O3"] <= TARGET_SLAG_SPEC["Cr2O3_max"] and slag["FeO"] <= TARGET_SLAG_SPEC["FeO_max"] and slag["SiO2"] <= TARGET_SLAG_SPEC["SiO2_max"] and slag["Al2O3"] <= TARGET_SLAG_SPEC["Al2O3_max"] and slag["CaO"] <= TARGET_SLAG_SPEC["CaO_max"] and slag["MgO"] <= TARGET_SLAG_SPEC["MgO_max"] ) # Ratios slag_ratio = (slag["MgO"] + slag["CaO"]) / slag["SiO2"] basicity = slag["CaO"] / slag["SiO2"] ratio_ok = ( abs(slag_ratio - TARGET_RATIOS["slag_ratio"]) <= 0.05 and abs(basicity - TARGET_RATIOS["basicity"]) <= 0.05 ) return metal_ok and slag_ok and ratio_ok

## 8.3 Usage Example

metal_pred = { "Cr": 58.2, "Si": 3.5, "C": 7.9, "P": 0.02, "S": 0.03 } slag_pred = { "Cr2O3": 6.5, "FeO": 1.4, "SiO2": 25.0, "Al2O3": 22.0, "CaO": 6.5, "MgO": 24.0 } if check_constraints(metal_pred, slag_pred): print("✅ Blend Accepted (58/4 grade achieved)") else: print("❌ Blend Rejected (Out of specification)")

# 9. COMPLETE PYTHON CLASS IMPLEMENTATION

Copy this complete class to calculate all KPIs in your application.

import pandas as pd import numpy as np class FerrochromeKPI: ''' Complete Ferrochrome KPI Calculator All calculations on per-ton / per-batch basis ''' def __init__(self, df, alloy_produced_kg=None, power_consumed_kWh=None): ''' Initialize with charge mix dataframe df columns: Material, Weight_kg, Cr2O3, Fe, SiO2, Al2O3, CaO, MgO, FC, H2O, Rate ''' self.df = df.copy() self.total_charge_kg = df['Weight_kg'].sum() self.alloy_kg = alloy_produced_kg self.power_kWh = power_consumed_kWh self._calculate_blended_values() def _calculate_blended_values(self): '''Calculate all blended (weighted average) values''' df = self.df total = self.total_charge_kg # Blended compositions self.blended_Cr2O3 = (df['Weight_kg'] * df['Cr2O3']).sum() / total self.blended_Cr = self.blended_Cr2O3 * 0.684 self.blended_Fe = (df['Weight_kg'] * df['Fe']).sum() / total self.blended_SiO2 = (df['Weight_kg'] * df['SiO2']).sum() / total self.blended_Al2O3 = (df['Weight_kg'] * df['Al2O3']).sum() / total self.blended_MgO = (df['Weight_kg'] * df['MgO']).sum() / total # CaO from flux only flux_df = df[df['CaO'] > 0] self.blended_CaO = (flux_df['Weight_kg'] * flux_df['CaO']).sum() / total if len(flux_df) > 0 else 0 # Fixed Carbon carbon_df = df[df['FC'] > 0] self.FC_kg = (carbon_df['Weight_kg'] * carbon_df['FC']).sum() / 100 if len(carbon_df) > 0 else 0 # Moisture self.H2O_kg = (df['Weight_kg'] * df['H2O']).sum() / 100 # Total reducible metal self.Cr_Fe_total = self.blended_Cr + self.blended_Fe # ============ CHARGE MIX KPIs ============ def get_blended_Cr2O3(self): return round(self.blended_Cr2O3, 2) def get_blended_Cr(self): return round(self.blended_Cr, 2) def get_blended_Fe(self): return round(self.blended_Fe, 2) def get_blended_SiO2(self): return round(self.blended_SiO2, 2) def get_blended_Al2O3(self): return round(self.blended_Al2O3, 2) def get_blended_MgO(self): return round(self.blended_MgO, 2) def get_blended_CaO(self): return round(self.blended_CaO, 2) def get_FC_kg(self): return round(self.FC_kg, 2) def get_H2O_kg(self): return round(self.H2O_kg, 2) def get_Cr_Fe_total(self): return round(self.Cr_Fe_total, 2) # ============ SLAG CHEMISTRY KPIs ============ def get_MgO_Al2O3_ratio(self): if self.blended_Al2O3 > 0: return round(self.blended_MgO / self.blended_Al2O3, 2) return 0 def get_basicity(self): if self.blended_SiO2 > 0: return round((self.blended_MgO + self.blended_CaO) / self.blended_SiO2, 2) return 0 def get_SiO2_CrFe_ratio(self): if self.Cr_Fe_total > 0: return round(self.blended_SiO2 / self.Cr_Fe_total, 3) return 0 def get_FC_CrFe_ratio(self): metal_kg = self.Cr_Fe_total * self.total_charge_kg / 100 if metal_kg > 0: return round(self.FC_kg / metal_kg, 3) return 0 # ============ COST KPIs ============ def get_blended_cost_per_ton(self): cost = (self.df['Weight_kg'] * self.df['Rate']).sum() return round(cost / (self.total_charge_kg / 1000), 2) def get_ore_cost_per_ton_alloy(self): if self.alloy_kg is None: return None ore_df = self.df[self.df['Cr2O3'] > 0] cost = (ore_df['Weight_kg'] * ore_df['Rate']).sum() return round(cost / (self.alloy_kg / 1000), 2) def get_reductant_cost_per_ton_alloy(self): if self.alloy_kg is None: return None carbon_df = self.df[self.df['FC'] > 0] cost = (carbon_df['Weight_kg'] * carbon_df['Rate']).sum() return round(cost / (self.alloy_kg / 1000), 2) # ============ EFFICIENCY KPIs ============ def get_Cr_recovery(self, alloy_Cr_percent=62): if self.alloy_kg is None: return None Cr_input = self.blended_Cr * self.total_charge_kg / 100 Cr_output = self.alloy_kg * alloy_Cr_percent / 100 return round((Cr_output / Cr_input) * 100, 2) if Cr_input > 0 else 0 def get_specific_power(self): if self.alloy_kg is None or self.power_kWh is None: return None return round(self.power_kWh / (self.alloy_kg / 1000), 0) def get_specific_ore(self): if self.alloy_kg is None: return None ore_df = self.df[self.df['Cr2O3'] > 0] return round(ore_df['Weight_kg'].sum() / (self.alloy_kg / 1000), 0) def get_specific_carbon(self): if self.alloy_kg is None: return None return round(self.FC_kg / (self.alloy_kg / 1000), 0) # ============ SUMMARY ============ def get_all_kpis(self): '''Return dictionary of all KPIs''' return { 'Blended_Cr2O3_%': self.get_blended_Cr2O3(), 'Blended_Cr_%': self.get_blended_Cr(), 'Blended_Fe_%': self.get_blended_Fe(), 'Blended_SiO2_%': self.get_blended_SiO2(), 'Blended_Al2O3_%': self.get_blended_Al2O3(), 'Blended_MgO_%': self.get_blended_MgO(), 'Blended_CaO_%': self.get_blended_CaO(), 'FC_kg': self.get_FC_kg(), 'H2O_kg': self.get_H2O_kg(), 'Cr_Fe_total_%': self.get_Cr_Fe_total(), 'MgO_Al2O3_ratio': self.get_MgO_Al2O3_ratio(), 'Basicity': self.get_basicity(), 'SiO2_CrFe_ratio': self.get_SiO2_CrFe_ratio(), 'FC_CrFe_ratio': self.get_FC_CrFe_ratio(), 'Blended_Cost_Rs_per_ton': self.get_blended_cost_per_ton(), 'Sp_Power_kWh': self.get_specific_power(), 'Sp_Ore_kg': self.get_specific_ore(), 'Sp_Carbon_kg': self.get_specific_carbon(), 'Cr_Recovery_%': self.get_Cr_recovery() }

# 10. QUICK REFERENCE TABLES

## 10.1 KPI Summary Table

| KPI | Formula | Target |
| --- | --- | --- |
| Blended Cr2O3 | Weighted Avg | 38-48% |
| Blended Cr | Cr2O3 × 0.684 | 26-33% |
| Cr/Fe Ratio | Cr / Fe | 2.8-4.5 |
| MgO/Al2O3 | MgO / Al2O3 | 1.2-1.8 |
| Basicity | (MgO+CaO) / SiO2 | 1.0-1.4 |
| SiO2/(Cr+Fe) | SiO2 / (Cr+Fe) | < 0.20 |
| FC/(Cr+Fe) | FC_kg / metal_kg | 0.85-1.05 |
| Cr Recovery | Cr_out / Cr_in | 85-92% |
| Specific Power | kWh / ton alloy | 3400-3800 |
| Slag Cr2O3 | Cr2O3 × (1-recovery) | < 8% |

## 10.2 Conversion Factors

| Parameter | Target Value |
| --- | --- |
| Cr2O3 to Cr | × 0.684 |
| SiO2 to Si | × 0.467 |
| Fe2O3 to Fe | × 0.70 |
| 1 inch | 1440 DXA |
| 1 kg H2O | ~0.7 kWh power |
| Base SP Power | 3200-3500 kWh/ton |

## 10.3 Grade Classifications

| Parameter | Target Value |
| --- | --- |
| HC FeCr (High Carbon) | 60-70% Cr, C ≤ 8% |
| MC FeCr (Medium Carbon) | 56-65% Cr, C ≤ 4% |
| LC FeCr (Low Carbon) | 60-65% Cr, C ≤ 0.5% |
| 58/4 Grade (BAL Standard) | 58±0.5% Cr, Si ≤ 4% |

--- End of Document ---

Balasore Alloys Limited | IT Department - Business Intelligence

Document maintained for operational excellence and digital transformation